## Slide 1
Multiphonon theory of electronic transitions at defects in semiconductors – carrier capture and H Release
Laura Nichols
November 2024
Committee
Sokrates Pantelides (advisor), VU
Andrew O’Hara
Collaborators (Vanderbilt)
Xiaoguang Zhang (co-advisor), UF
William Perry (graduate student)
Guanzhi Li (graduate student)
Schrimpf-Fleetwood-Reed Radiation
Effects and Reliability Group
Kalman Varga, VU
Ron Schrimpf, VU
Sait Umar, VU
Xiaoguang Zhang (co-advisor)
Collaborators (Florida)
Yue Yu (former student)
Collaborators (UT Dallas)
Max Fischetti
Dallin Nielsen (post-doc)

## Slide 2: Background

## Slide 3: Semiconductor applications

## Slide 4: Si MOSFET vs GaN HEMT
M. N. A. Aadit et al., InTech (2017)
Notes: MOSFET set up through junctions between differently-doped Si
HEMTs, however use a junction between materials of different band gaps to set up a conduction channel without dopants that can scatter carriers
HEMTs are also made from material with a larger band gap, which makes them more suitable for high-temperature/high-power applications
Si-based MOSFETs are primarily used now because Si can be made very cleanly made relatively cheaply compared to other semiconductor devices
The production process can be tuned to avoid certain defects, but we need more information on which defects cause the most degradation

## Slide 5: Effect of Defects
Notes: In both devices, H is present during the fabrication process and passivates defects

## Slide 6: Radiative Capture
DE
e
Capture
Energy
Conduction band
Valence band
Notes: Base of the theory is based on Fermi’s golden rule that gives the probability of transition between two states
That theory must be expanded to cover both the electronic and the vibrational state because we consider nonradiative transitions and energy must be conserved
We use the Born-Oppenheimer approximation that says that the electronic transition happens much quicker than the atoms move so that they can be considered to be stationary during the transition
FGR and BOA are well-known. We start with the specific case of capture, where there is a single final state and a well-defined change in the equilibrium positions before and after displacement. Seems straightforward.

## Slide 7: Nonradiative Scattering
e
Scattering
Energy
Conduction band
Valence band
Public Domain; Sean Kelley via NIST
DE

## Slide 8: Nonradiative Scattering
e
Scattering
Energy
Conduction band
Valence band
Public Domain; Sean Kelley via NIST
DE

## Slide 9: Engineering-Level Models
Y. Puzyrev et al., IEE Trans. Elec. Dev. (2014)
M. Bina et al., IEE Trans. Elec. Dev. (2014)
Notes: Focused on defects in semiconductors like dangling bonds and Ga vacancies
Hydrogenated during fabrication to make benign
Can be activated through hydrogen release

## Slide 10: Energy Transfer via Scattering and Capture
Inelastic Scattering
DE
e
Energy
Conduction band
Valence band
DE
e
Capture
Energy
Conduction band
Valence band
Notes: Base of the theory is based on Fermi’s golden rule that gives the probability of transition between two states
That theory must be expanded to cover both the electronic and the vibrational state because we consider nonradiative transitions and energy must be conserved
We use the Born-Oppenheimer approximation that says that the electronic transition happens much quicker than the atoms move so that they can be considered to be stationary during the transition
FGR and BOA are well-known. We start with the specific case of capture, where there is a single final state and a well-defined change in the equilibrium positions before and after displacement. Seems straightforward.

## Slide 11: Nonradiative capture

## Slide 12: Problem complexity
Converge usual parameters and wave function overlaps
Calculations scale as
Must determine best atomic positions to calculate overlaps at
Results can be very sensitive to energy dissipated into phonons

## Slide 13: Previous Approximations
G. Barmparis et al., Phys. Rev. B (2015)
A. Alkauskas et al., Phys. Rev. B (2014)
Notes: Alkauskas et al. allowed the frequency to change between modes, but they approximated the initial and final states each to a single average mode dominated by the defect vibrations
Barmparis et al. allowed all modes to participate, but they assumed that the initial and final frequencies were the same, had to sample the modes allowed to participate at a time, and couldn’t compute the electron-phonon coupling term

## Slide 14: Example Timing of All Modes and Optimization
4x4x4, 512-atom Si supercell
VASP DFT: 25 node-minute SCF per k-point (linear scaling with nodes)
Code to get transition rate:
Time to get wave function derivatives:
days, node hours
1.25 node hours per k-point (not fully parallelized)
8 node minutes per k-point (linear scaling with nodes)
days, node hours
Notes: Can’t utilize symmetry with the defects we consider
DFT calculations scale as O(N^3)
When considering all modes, we have to calculate wave function derivatives for each mode, scaling with O(N)
Supercell must be roughly cubic, so increasing supercell size scales number of atoms cubically

## Slide 15
VSi-H3
GaN-CN
Capture paper under review
Nonequilibrium
Equilibrium
Notes: Box represents multiple samples
They reported data for all of the samples in one paper, but not enough for us to reconstruct what we have on the plot, so we had to go to different papers to compile the information we needed
More experiments are needed

## Slide 16: H Release Theory

## Slide 17: Energy Transfer via Capture and Scattering
Ec
Ev
DE
e
Ec
Ev
DE
e
Inelastic Scattering
Capture
Notes: With the nonequilibrium capture theory created and illustrated, we can generalize to scattering
Key parameter needed for our theory is a displacement between the initial and final equilibrium positions that can be projected onto the phonon eigenvectors
It is commonly thought that there is no displacement for band-to-band scattering
In capture, only a single displacement due to the change in the charge state of the defect is considered; differences between the band states are neglected

## Slide 18: Capture vs Scattering
Generalized coordinate
Total Energy
Generalized coordinate
Total Energy
Inelastic Scattering
Capture

## Slide 19: Capture vs Scattering
Generalized coordinate
Total Energy
Generalized coordinate
Total Energy
Inelastic Scattering
Capture

## Slide 20: Change in Charge Density Distribution

## Slide 21: Resonance States
Ec
Ev
Bonding
Antibonding
A. O’Hara et al., Preprint (2024)
Notes: Resonances like the bond and antibonding states could also contribute
These resonances have to be searched for

## Slide 22: H Release Algorithm
Ec
Ev
e
Inelastic Scattering
Split across modes
Average over final states using FGR
Average over initial states using
Get average rate of energy transfer to each mode
Step in time to get new occupations

## Slide 23: Rogue Waves
Rare large displacements may contain much of the probability of an event.
Approximations good for typical configurations may miss this contribution.
Vs.
Slide from W. Perry and X.G. Zhang, UFL
Rogue-Waves
Monte Carlo
Exceedance Probabilities

## Slide 24
Exceedance Probabilities

## Slide 25
Exceedance Probabilities

## Slide 26
Exceedance Probabilities
Assume constant temperature
Get rate from change in probability

## Slide 27: Connection to Experiments
New algorithm
S. Mukherjee et al., IEE Trans. Elec. Dev. (2016)

## Slide 28: Search for Model Defect
Amorphous SiO2 increases computational cost
ON:H metastable configuration
Conduction bands in GaN require many k-points
NGa antisite defect complex formations
Plot from Materials Project

## Slide 29: Proof-of-Concept Calculation

## Slide 30: Device Specifications
Carrier densities and schematic from D. Nielsen and M. Fischetti, UT Dallas
I
I
III
II
Notes: I = lowest field, highest density (black)
II = highest field (gold)
III = middle field (blue)
Field and carrier densities come from a HEMT device
Valence bands are then modeled to get probability distribution

## Slide 31: Rate of Release

## Slide 32: Fraction of Activated Defects Over Time

## Slide 33: Fraction of Activated Defects Over Time
S. Mukherjee et al., IEE Trans. Elec. Dev. (2016)

## Slide 34
(a)
(b)

## Slide 35: Arrhenius Plot
Best fit:

## Slide 36: Code Transfer
Capture, scattering, and H release fully implemented
Two-day workshop held at Vanderbilt with Dallin, Andy, and Xiao
Future applications
Capture at various defects
Integration with Boltzmann code
Application to H release in real devices